PRODUCT DATA SHEET
Coping profile for parapit walls / roofs 240mm-660mm, Coping widths  
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	Designation
	Coping profile for parapet walls / roofs

	Description
	Aluminium coping, polyester powder coated 

	Product area
	Roof

	Product category
	Coping

	Material 
	2mm aluminum, polyester powder coated 

	Length
	3000 mm

	Customs tariff number
	76042990

	
	
	

	[bookmark: _Hlk215840548][bookmark: _Hlk215843780]Code 
	Dim A (mm)
	Wall width range (mm)
	Material thickness (mm)

	CAP-STR-240
	240
	150-180
	2.0

	CAP-STR-300
	300
	180-240
	2.0

	[bookmark: _Hlk215843617]CAP-STR-360
	360
	240-300
	2.0

	 CAP-STR-420
	420
	300-360
	2.0

	CAP-STR-480
	480
	360-420
	2.0

	CAP-STR-540
	540
	420-480
	2.0

	 CAP-STR-600
	600
	480-540
	2.0

	CAP-STR-660
	660
	540-600
	2.0





Retention brackets are required to secure the copings in place. Please note that retention brackets are sold separately. 
Please refer to retention bracket data sheet for more information.

This product data sheet reflects the current stage of development of our products and will be superseded upon release of a newer edition. Please ensure you are referring to the most up-to-date version of this document.

Our warranty and liability obligations apply only to goods supplied in accordance with our current terms and conditions of sale. Please follow all relevant installation, application, and storage guidelines when using this product.

All information is provided without guarantee and is subject to technical modification without prior notice. Product images are for illustration purposes only and may differ from the product supplied.

Please dispose of all materials responsibly and in accordance with UK environmental regulations.
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